2025 Bachelor’s Graduation Thesis

Development of a CAM System for Incremental Forming of CFRTP from 3D CAD Data

Precision Engineering Research Group

Green Engineering and Applied Sciences Course

Faculty of Science and Technology

Sophia University

A2177802

Karter Wong

Guidance Professor Hidetake Tanaka

Submitted on 17 July 2022

Table of Contents

Chapter 1: Introduction	5

1.1 Background information: Incremental Forming	5

1.1.1 Development History	5

1.1.2 Types of Incremental Forming	5

Single Point Incremental Forming (SPIF):	6

1.1.3 Current and Potential Applications for Incremental Forming	6

1.2 NC Machine Tools	9

1.2.1 Overview	9

1.2.2 NC program, G-Code, and Functions	9

1.2.3 3D CAD	9

1.2.4 CAM	10

1.2.5 Python	10

1.2.6 Toolpath	11

1.3 CFRP (Carbon Fiber Reinforced Plastic)	11

1.3.1 Overview	11

1.3.2 Classification and Characteristics of CFRP	12

1.4 Previous Research A	12

1.4.1 Overview	12

1.4.2 CAM System and Design of the Test Shape	12

1.4.3 Experimental Equipment	13

1.4.4 Results	13

1.4.5 Conclusions	14

1.5 Current Research Objectives	14

Chapter 2: Toolpath Generation	15

2.1 Program Overview	15

2.2 Libraries and Variables	15

2.3 Modules	17

Loading STL File and Extracting Point Cloud	17

Filtering Close Points to Prevent Clustering	18

Sorting Points to Prevent Doubling Back	18

Smoothing Hull Points	19

Applying Reverse Offset	20

2.4 Toolpath Generation Process	21

Main Toolpath Generation Loop	21

2.6 G-Code Generation and Export	24

2.7 NC Viewer Confirmation	27

Chapter 3: Incremental Forming Experiment and Evaluation	28

3.1 Introduction	28

Experimental Equipment	28

Machining Center	29

Discontinuous CFRTP	29

Oil Bath	30

Type of Oil	30

Forming tool	31

Aluminum and Carbon Fiber molds	31

Jig Dimensions	32

Test shape	33

3.3 Experimental Setup and Procedure	33

3.4 Experimental Results	34

CAM System Comparison	34

Incremental Forming Experiments	34

3.5 Evaluation	36

Chapter 5: Conclusion and Future Improvements	37

Appendix	38

Chapter 6: References	52

# Chapter 1: Introduction

## 1.1 Background information: Incremental Forming

The increasing demand for lightweight, durable, and reusable materials in modern products has highlighted Carbon Fiber Reinforced Plastics (CFRP)due to its high strength-to-weight ratio and excellent mechanical properties [10]. Traditional molding techniques, while efficient for high-volume production, are too costly for low-volume and complex-designed products [2]. The low volume production, in addition to the mold costs, increases manufacturing and consumer costs, limiting accessibility. Dieless forming methods, such as 3D printing and incremental forming, offer a potential solution to produce low-volume products by eliminating the need for molds while allowing for the manufacturing of complex shapes [2]. The exceptional properties of CFRP make it challenging to manufacture products using innovative techniques, such as incremental forming, to address the challenges of manufacturing low-volume, high-mix production [2].

### 1.1.1 Development History

Incremental forming, pioneered in Japan during the 1990s by researchers such as Matsubara [14], is a dieless manufacturing technique designed for low-volume, complex components. Unlike traditional molding, it deforms materials through localized, incremental tool movements, offering flexibility for prototyping and custom production [2]. The process encompasses a variety of different techniques and methods, but the key characteristics of this type of manufacturing technology include:

- High geometric flexibility for complex shapes

- Elimination of dedicated molds

- Suitability for thin-shell structures

- Enhanced forming limits for sheet materials

- Cost-effective production for low-demand components

### 1.1.2 Types of Incremental Forming

There are many types of incremental forming; however, most are categorized into three main categories: Single Point Incremental Forming (SPIF), Two Point Incremental Forming (TPIF), and Double-Sided Incremental Forming (DSIF). For this research paper, single-point incremental forming was employed; therefore, two-point and double-sided incremental forming will not be discussed in the following sections as they are not relevant to the research paper.

### Single Point Incremental Forming (SPIF)

Single-point incremental forming is the most straightforward and economical variant, where a tool deforms the sheet incrementally without the need for a mold. A backing plate often supports the workpiece or sheet of material. The process is highly flexible, allowing for rapid prototyping and low-volume production, as it can be executed on conventional CNC machines without the need for hydraulic presses. SPIF is ideal for creating parts directly from CAD models, eliminating the need for male or female dies. However, it may suffer from reduced accuracy due to springback and longer forming times. Applications include prototyping and small-batch production, with studies highlighting its increased formability but lower final accuracy [2].

Figure 1: Principle of Single Point Incremental forming [Iseki et al., 1989].

### Two-Point Incremental Forming (TPIF)

Two-Point Incremental Forming (TPIF) enhances the SPIF process by adding a supporting die—either partial or full—beneath the sheet metal. The forming tool presses the sheet against this die, which provides additional stability and control during deformation. This setup improves dimensional accuracy and surface quality compared to SPIF, as the die helps reduce springback and ensures the sheet conforms more closely to the intended shape. TPIF is particularly valuable for producing parts with tighter tolerances or detailed features, making it a good fit for applications like automotive panels or aerospace components where precision is critical. The trade-off, however, is the need to design and manufacture the die, which increases tooling costs and setup time. This makes TPIF less ideal for one-off prototypes but more practical for small-to-medium production runs where the improved part quality can justify the investment in a die.

### Double-Sided Incremental Forming (DSIF)

Double-Sided Incremental Forming (DSIF) takes incremental forming a step further by using two synchronized tools—one on each side of the sheet metal. These tools work together to deform the sheet simultaneously, applying forces from both directions. This dual-tool approach enhances formability, allowing for more complex shapes and reducing residual stresses that might occur in single-sided methods. DSIF can also speed up the forming process and minimize defects like wrinkling or tearing, especially in materials with low ductility. It’s particularly promising for high-strength materials or intricate parts used in aerospace or defense industries. However, DSIF’s complexity is a drawback: it requires precise coordination between the tools, often necessitating advanced equipment like dual-robot systems or specialized CNC machines. This increases both the cost and the technical skill required, making DSIF better suited for advanced manufacturing scenarios rather than simple prototyping.

### 1.1.3 Current and Potential Applications for Incremental Forming

Incremental forming's ability to efficiently and cost-effectively manufacture complex shell shapes makes it ideal for low-volume, high-mix manufacturing, particularly in prototyping, custom component production, and material testing [2]. By eliminating the need for dedicated molds, incremental forming reduces setup costs and lead times, enabling rapid production and customization across various industries. Its ability to produce complex shapes with high forming limits enables incremental forming as a solution for applications requiring lightweight, durable components, especially when using advanced materials like Carbon Fiber Reinforced Thermoplastics (CFRTP) [2].

The broad applications of incremental forming underscore its potential to change the way we manufacture products on a large scale, particularly for components made from materials that are harder to manufacture with traditional methods. By enabling the cost-effective production of complex, lightweight parts, the technique supports sustainability goals across various industries, aligning with global trends toward reduced emissions and increased resource efficiency [15].

#### Automotive Industry

In the automotive sector, incremental forming has seen an increase in adaptation for low-volume production of complex, lightweight components, aligning with the industry's shift toward sustainable and efficient manufacturing [6]. For example, Toyota Motor Corporation utilizes static incremental forming to fabricate the front bumper of the Lexus LC Edge, achieving precise shaping without the use of molds, which reduces production costs by approximately 30% compared to traditional molding for low-volume runs [6]. The bumper, constructed from discontinuous CFRTP, leverages the high press formability to achieve a smooth surface and dimensional accuracy of ±0.1 mm [6]. Similarly, Ford utilizes incremental forming for custom interior panels in the Mustang Mach-E electric vehicle, enabling the rapid prototyping of lightweight dashboard components with complex curvatures and reducing the component's weight by 15% compared to aluminum alternatives [6]. Nissan applies the technique for structural components in the Leaf electric vehicle, such as battery enclosure supports, which benefit from CFRTP's vibration absorption and corrosion resistance, enhancing vehicle range by 5% through weight reduction [6]. These applications demonstrate the incremental forming process's ability to meet stringent automotive requirements for weight, strength, and cost efficiency.

Figure 2: Incremental Forming Application in Lexus LC Edge Front Bumper [Toyota Motor Corporation, 2020].

#### Aerospace Industry

#### In the aerospace sector, SPIF is employed for prototyping and fabricating lightweight, high-strength components that can also reduce the vibration in aircraft and complex structural parts. Incremental forming's ability to machine materials such as titanium and aluminum alloys, which are prevalent in the aerospace industry, makes it suitable for producing parts with strict performance requirements. Studies suggest that SPIF has the potential to form intricate aerospace components, such as wing parts or fuselage sections, contributing to weight reduction and improved fuel efficiency in aircraft design [15]. These applications highlight the potential for SPIF to be used in the aerospace industry.

#### Medical Applications

SPIF is utilized in the medical field for the manufacturing of customized implants, including cranial and craniofacial implants, where precision is critical. SPIF enables the creation of complex, patient-specific geometries using materials such as titanium. A study by Duflou et al. (2013) demonstrated the application of SPIF in producing accurate titanium craniofacial implants with high forming angles, meeting medical standards for fit and functionality [2]. Other research has explored SPIF for thin-shell clavicle implants, highlighting the versatility of SPIF in medical device manufacturing [4]. The capabilities of SPIF improve outcomes for patients in reconstructive and orthopedic surgeries. SPIF's precision and material versatility make it a critical tool in advancing medical device manufacturing.

## 1.2 NC Machine Tools

### 1.2.1 Overview

Numerical Control (NC) machines execute automated operations via programmed numerical commands, controlling tool position, speed, and operations with high precision [9]. Unlike manual processes, NC automation reduces processing times, enhances productivity, and lowers labor costs. Computer Numerical Control, or CNC, is an advanced form of numerical control that utilizes computer systems to manufacture products accurately, making it a prevalent technology in modern manufacturing [9].

### 1.2.2 NC program, G-Code, and Functions

An NC program automates CNC machine operations through blocks of code, such as:

G01 X8 Y10 Z9;

Each block comprises a preparatory function section (e.g., G01 for linear interpolation) and a coordinate section (e.g., X8 Y10 Z9 for tool position). Codes that start with the letter “G” serve as preparatory functions, M-codes handle miscellaneous functions (e.g., spindle start/stop), F-codes set feed rates, and S-codes control spindle speed [9]. Table 1 lists the functions used in this research.

Table 1: G-Code Functions for Incremental Forming

| G-Code | Positioning | G00 |
| --- | --- | --- |
|  | Linear Interpolation | G01 |
|  | mm input | G21 |
|  | Absolute coordinate command | G90 |
|  | Relative coordinate command | G91 |
|  | Work coordinate system settings. | G92 |
| M Code | Spindle section | M03 |
|  | Program end | M30 |
| F Code | Feed Speed (mm/min) | F1000 |
| S Code | Rotation Speed (RPM) | S500 |

### 1.2.3 3D CAD

Computer-Aided Design (CAD) software enables precise digital design of components [7]. Unlike 2D CAD, 3D CAD, such as Creo Parametric 4.0 used in this study, supports complex geometries and prototyping, reducing production errors by enabling the accurate generation of STL files for toolpath creation [7]. All test pieces and molds in this research were designed using 3D CAD to ensure precision in incremental forming.

Figure 3: 3D CAD Model of Test Piece Designed in Creo Parametric [Wong, 2025].

### 1.2.4 CAM

Computer-aided manufacturing (CAM) systems utilize software and computer-controlled machinery to automate the manufacturing process. CAM systems are used to generate machining programs for CNC machines, automating the creation of toolpaths and reducing errors [7]. By simulating the generated toolpaths before forming, issues on the toolpath can be identified and fixed before manufacturing, significantly lowering production time and costs [7]. In this study, the CAM system processes STL files from Creo Parametric to produce the NC program for incremental forming.

G90 ; (Absolute positioning)

G21 ; (Set units to millimeters)

G92 X0.0 Y0.0 Z0 ; (Set workpiece origin)

F1000 ; (Set feed rate)

G01 X0.0 Y0.0 Z20 ; (Move to safe height)

Figure 4: Sample NC program for Incremental Forming [Wong, 2025].

### 1.2.5 Python

Python, an open-source programming language, is renowned for its simplicity, and its libraries enable programmers to develop complex programs efficiently [3]. Libraries such as NumPy, Pandas, and PyVista can efficiently process large amounts of data, making Python an ideal choice for developing CAM systems [3]. In this study, Python was selected for its readability and ability to process STL files and generate optimized G-code toolpaths for incremental forming.

### 1.2.6 Toolpath

A tool path is the path along which a machining tool moves. A tool path is created using the 3D coordinates of an STL file from CAD software to collect all the points, forming a point cloud from the triangles of the STL file. From this, the points are sorted, duplicate points are deleted, a set of coordinates is generated, and then the necessary pieces are added to convert the coordinates into the NC program. The NC program can instruct the tool on the machining path. The toolpath was viewed using an NC viewer web browser to identify potential issues before manufacturing.

Figure 5: Toolpath Visualization for Truncated Cone [Wong, 2025].

## 1.3 CFRP (Carbon Fiber Reinforced Plastic)

### 1.3.1 Overview

Carbon Fiber Reinforced Plastics (CFRP) combine carbon fibers with a polymer matrix to achieve superior mechanical properties, including a specific strength up to 10 times that of iron and a specific gravity of 1.8 g/cm³, which is significantly lower than that of aluminum 2.7 g/cm³ [10]. CFRP's high strength-to-weight ratio, vibration absorption, and corrosion resistance make it ideal for use in various industries that emphasize the use of lightweight and durable materials, such as aerospace, automotive, sports equipment, and medical devices [10].

### 1.3.2 Classification and Characteristics of CFRP

CFRP is categorized by matrix type and fiber orientation, influencing its mechanical properties and applications [10]. The four main properties are Thermosetting (CFRTS): Thermoplastic (CFRTP), continuous fiber, and discontinuous fiber CFRP. CFRTS is characterized by a high specific strength and heat resistance. However, it requires long molding times and is non-recyclable [10]. CFRTS is used in the aerospace industry and sports equipment. CFRTP offers lower specific strength and heat resistance but enables shorter molding times, lower costs, and partial recyclability [10]. Continuous Fiber CFRTP features a layered structure with aligned fibers, providing high specific strength but limited formability [10]. Discontinuous Fiber CFRTP features a random fiber

orientation, providing isotropic strength and high press formability, which makes it ideal for complex shapes despite its lower overall strength [10].

## 1.4 Previous Research A

### 1.4.1 Overview

In this previous research, the researcher developed a Python-based CAM system for static incremental forming of discontinuous fiber CFRTP, utilizing an oil bath for material heating to enable dieless forming. The system generates NC program toolpaths from CAD models, addressing the high costs and inflexibility of traditional molding for low-volume, thin-shell components [5].

### 1.4.2 CAM System and Design of the Test Shape

The CAM system achieves three goals: reading an STL file from Creo Parametric 4.0, extracting the 3D point clouds of the target shapes, and creating a tool path in G-code [5]. The code utilizes Python libraries to generate a point cloud from the STL file. It converts the clouds into layers by Z-height and connects the points in each layer by the minimum Euclidean distance. Finally, it takes the coordinates and adds the proper syntax for use by the CNC machines. The shape created in Creo was a truncated cone with varying dimensions. The radius of the shape ranges from 20 mm to 40 mm, and similarly, the wall angle is 30°, 40°, and 50°. The pitch or resolution of the STL is 1. The dimensions were selected to match the working area and limitations of the experimental setup. The shape was chosen because it is suitable for proof of concept, especially for plastic deformation layering [5].

### 1.4.3 Experimental Equipment

The experimental setup for this research is summarized in Table 2, with most equipment reused for consistency and reproducibility.

Table 2: Experimental Equipment Specifications

| Equipment | Description | Specification |
| --- | --- | --- |
| CFRTP Sheet | PA6 matrix, 20 wt% carbon fiber | 110 mm × 110 mm × 1 mm |
| Oil Bath | T-22H (Thomas Scientific) | Up to 200°C, ±0.2°C precision, jet circulation |
| Silicone Oil | KF968 (Shin-Etsu) | Non-volatile, stable to 250°C, fire-resistant |
| CNC Machine | Sodick MC430L | X 420 mm, Y 350 mm, Z 200 mm, feed up to 36 m/min |
| Tool (Mandrel) | SUS304 | 5 mm diameter, 2.5 mm radius tip, 60 mm length |
| Jig | Custom design | Submerged in oil bath, secure clamping, detachable |

### 1.4.4 Results

The experiments identified key parameters that influence the success of incremental forming, including material temperature, tool rotation, wall angle, and radius [5].

Temperature Effects

Optimal forming occurred at 180–200°C (453–473 K), achieving smooth surfaces and minimal defects. Below 160°C (433 K), insufficient softening led to cracks, with a minimum forming temperature of 50°C (323 K) [5].

Tool Rotation

A spindle speed of 1000 rpm enhanced forming depth (up to 14.9 mm) and surface smoothness (Ra < 2 µm), reducing uneven wall thickness compared to non-rotating conditions [5].

Wall Angle

Wall angles of 30° and 40° yielded smooth forming with minimal springback (< 5%). Angles near 40° exhibited minor deformations, while angles greater than or equal to 50° were at risk of cracking due to excessive stress [5].

Radius Variations

Smaller radii (20 mm) achieved deeper forming (14.9 mm) but increased wall stress (up to 300 MPa), while larger radii (40 mm) produced shallower forms (8 mm) with uniform wall strength [5].

Table 3: Forming Criteria Summary

| Condition | Depth (mm) | Temperature (°C) | Radius (mm) | Wall Angle (°) | Spindle Speed (rpm) |
| --- | --- | --- | --- | --- | --- |
| Maximum | 14.9 | 200 | 20 | 40 | 1000 |
| Minimum | 3.6 | 160 | 40 | 50 | 0 |

### 1.4.5 Conclusions

Previous research [5] developed a Python-based CAM system that effectively generates toolpaths from STL data for use in static incremental forming of discontinuous CFRTP. By leveraging Python libraries such as PyVista, Pandas, and NumPy, the CAM system extracted a 3D point cloud, sorted them by Z-height, and connected points using a nearest-neighbor algorithm, enabling flexible production of complex shapes for low-volume applications [5]. This approach to creating a toolpath enables the CAM system to be compatible with any CAD software that can produce STL files, thereby streamlining the process from design to manufacturing. However, the CAM system itself has several limitations, preventing it from handling complex geometries and is susceptible to toolpath errors, such as creating a "messy" toolpath that moves the tool to unnecessary points.

During the incremental forming experiments, it was found that wall angles of 50° or greater had a higher chance of breaking the test piece [5]. The Author of previous research A highlighted some challenges for future experiments, namely the issue of springback shape distortion and the need for advanced evaluation methods, suggesting that including scribed circle tests and 3D scanning with Einscan-SE might help with analyzing the formed shape [5].

## 1.5 Current Research Objectives

This study aims to enhance the CAM system by building upon previous research, as outlined in the appendix. The primary areas of focus for the CAM system are its ability to produce precise, error-free toolpaths for the static incremental forming of discontinuous CFRTP, the speed at which the program can output the Toolpath, and streamlining the process from design to manufacturing. To evaluate the CAM system’s ability to generate an error-free toolpath, the Toolpath's performance will be first presented in an NC viewer to confirm a clean toolpath and then tested using a Sodick MC430L CNC machining center in controlled heating conditions, with an oil bath at 120°C. The research will utilize the CAM system from previous research as a baseline for the new complex test shape, which will be presented later in the paper.

# Chapter 2: Toolpath Generation

## 2.1 Program Overview

This chapter describes the changes and overall flow of the updated CAM system, based on previous research, to enable the system to support complex geometries. The updated CAM system’s overall workflow is similar to that of the previous CAM system; it takes STL data from CAD software, generates a toolpath, and converts it to G-code for CNC machining [5]. The updated workflow introduces a step where all the logic for making the Toolpath is done. The entire CAM system is outlined in Section A1 of the appendix.

Figure 6: CAM System Workflow for Toolpath Generation [Wong, 2025].

## 2.2 Libraries and Variables

#### Libraries

Python libraries are collections of pre-written code that provide reusable functions and tools to simplify programming tasks. Libraries help optimize code that is used for computational problem-solving, simulations, and optimization [3]. Python offers an extensive library and the ability for third-party programmers to create libraries that are made publicly available.

The updated CAM system uses several libraries to optimize the Toolpath's generation.

- Pandas: This library is primarily utilized for data manipulation and storage. Pandas provides the `DataFrame` structure, which can store point cloud data extracted from STL files. Its ability to manage large datasets efficiently is crucial for processing the hundreds of thousands of points typically generated from 3D models [3].

- NumPy: Numpy can do high-performance numerical operations, including array manipulations and linear algebra functions. NumPy's efficiency is crucial for handling the computational demands of toolpath generation, ion as it can calculate the distances between points [3].

- SciPy (ConvexHull): The `ConvexHull` module from SciPy computes the convex hull of 2D point sets. It identifies the outermost points of each layer to define the toolpath boundary [3]. The function of the library ensures that only the external contour of the shape is machined, reducing unnecessary tool movements.

- STL (numpy-stl): The `mesh` module from the `numpy-stl` library reads STL files, extracting the point's coordinates to form the point cloud used for toolpath generation [7]. STL files are standard in CAD systems for representing 3D geometries as triangular meshes.

#### Variables

The previous CAM system also had variables. However, their primary function was to store values for the toolpath generation. In the updated CAM system, several variables were added to allow the operator to adjust the values according to the shape being created easily. The following variables are important to change depending on the test shape.

- TOOL_DIAMETER: The tool diameter variable, as the name suggests, is the diameter of the forming tool. This parameter is used to calculate the offsets, ensuring the tool's geometry is accounted for during forming [5]. The use of diameter is for simplicity, as the program can halve the value for the radius.

- Z_SPRINGBACK_OFFSET: When conducting incremental forming without a mold, the material often rebounds slightly; this phenomenon is called springback [12]. This variable typically has a negative value, which shifts the Z-coordinates down, thereby ensuring that the shape is machined correctly.

- LAYER_THICKNESS: During the incremental forming process, it is important to maintain uniform layer thicknesses. Uniform layer distances will improve the formability of the formed shape, this variable defines the vertical distance between layers, controlling the resolution of the Toolpath along the Z-axis. Uniform layer spacing ensures consistent forming depth [5].

- MIN_DISTANCE: The minimum distance variable is used to prevent clusters of points from forming along the Toolpath. This ensures that the Toolpath is smooth and prevents unnecessary tool movements [5].

- Z_OFFSET: This offset adjusts the Z-coordinate of the entire Toolpath to align with the CNC machine's workspace, ensuring the tool operates within the safe working area [9].

- SAFE_Z_RELATIVE: This variable specifies the height to which the tool retracts after forming, preventing collisions during tool withdrawal that might damage the machined shape [9].

## 2.3 Modules

The majority of the changes made to the CAM system are located in the setup of variables, libraries, and logic section of Figure 6. In that section, the code can be broken down into several subsections or modules. The modules are designed in this way so that the points are in a refined state before being run through the main toolpath loop or setting up the logic to be used in the main toolpath loop. The sections of code that are being referenced can be found in the appendix in order from section code A4 to A9.

### Loading STL File and Extracting Point Cloud

This module reads the STL file and converts its vertices into a structured point cloud, assigning them Cartesian coordinates (X, Y, and Z) for toolpath generation. The module then edits the point cloud to ensure that the layers grouped by the Z coordinate are equidistant to each other. The code accomplishes this by rounding the Z coordinate value to the nearest multiple of the layer thickness that was previously set. The module then removes duplicate points and incomplete coordinates to enhance computational efficiency and toolpath accuracy, which is key when processing complex geometries [5]. Then, the points are saved into a data frame for later use. You can see the section of code in the code A4 section of the appendix.

### Filtering Close Points to Prevent Clustering

This module sets up some logic to be used in the main toolpath generation loop. The module reduces the point density in the point cloud to remove clusters of points, which could lead to inefficient toolpaths or machining errors. The module accomplishes this by loading the points output from the previous module, calculating the distance from the initial point in the list of points, and removing any point that exceeds the min_distance value. The filtered points are returned as a NumPy array, preserving only points that are spaced apart. By enforcing a minimum distance, this function optimizes the Toolpath, reducing machining time while also reducing errors.

Figure 7: Toolpath Without the Clustering Function

### Sorting Points to Prevent Doubling Back

This module sorts points in each layer to create a non-overlapping, clockwise toolpath, minimizing travel distance and preventing toolpath intersections. The module calculates the mean of the points and determines the centroid of the layer. The layer's centroid then serves as a reference for calculating the angles of each point. The module sorts the points by these angles, reversing the order of points if there are any intersections between the lines it temporarily creates to prevent doubling back.

The sorting algorithm, inspired by a simplified Traveling Salesperson Problem (TSP) approach, ensures an efficient and non-overlapping toolpath, which is critical for smooth CNC operation and high-quality surface finishes [3]. By preventing doubling back, it reduces machining time and mitigates risks of toolpath errors, aligning with the research's goal of optimizing toolpath generation for complex CFRTP shapes [5].

Figure 8: Example of Doubling Back

### Smoothing Hull Points

To ensure a smooth machining process, this module is applied to points that are run through the convex hull function and the reverse offset module, making the transitions uniform and improving toolpath continuity. The module creates a copy of the points it is given and then computes a weighted average using the current point and the average of the neighboring points. The `alpha` parameter controls the smoothing intensity, balancing the original point's position with the influence of its neighbors. Then, the module ensures that the points are continuous and finally returns the points to the Toolpath.

Sharp transitions in the Toolpath can cause abrupt tool movements, leading to material fractures or tool vibrations. The smoothing module enhances the toolpath quality, ensuring uniform deformation.

Figure 9: Example of Sharp Layer Transitions

### Applying Reverse Offset

Reverse offset is a way to adjust the toolpath of a machine to account for the dimensions of the machining tool. This method takes into account the geometry of the shape as well the dimensions of the machining tool to accurately calculate where to tool should for the machined product is to the dimensions of the designed product as seen in figure X below.

The reverse offset module in this case, adjusts the Toolpath to account for the tool's geometry and material springback, ensuring accurate forming. During this process, the center of the tool is calculated from the points being processed in the main toolpath generation loop, defining the layer's shape. Then, the tool diameter and z_springback_offset values are applied to the points on the Toolpath to ensure that the machined shape is accurate. Finally, the adjusted 3D points are returned, incorporating the offset and smoothing.

Figure 10: Reverse Offset Method

## 2.4 Toolpath Generation Process

### Main Toolpath Generation Loop

The main loop integrates all previous functions to create a cohesive toolpath that can later be converted to G-code. The loop processes the point cloud by every Z-level or layer of the STL file to create a continuous toolpath. The loop begins by creating an empty list where the Toolpath will be stored after it is generated from the coordinates.

The loop will also keep track of the last point for smooth layer transitions and closing the layer. For the first layer in the shape, the point closest to the centroid is selected as the starting point. For the subsequent layers, the point that is closest to the last point of the previous layer is chosen. The loop starts processing the layers from top to bottom, mimicking the incremental forming process [2]. The loop calculates the centroid for the layer, using 5 points, to ensure sufficient data for the convex hull computation. Next, the convexhull identifies the outermost points of the 2D layer, defining the layer for machining [3]. After convexhull is applied, all the modules previously discussed, except for the STL loading and point cloud formation, are applied to the list.

Finally, the loop stores the processed layer in the list that it created at the beginning of the process, and the last point in the list is set as the first point for the next layer.

The use of uniform Z-levels and convex hulls ensures compatibility with CNC machining. At the same time, the selection of nearest-neighbor start points optimizes tool travel, reducing machining time and enhancing efficiency [3]. The robust error handling aligns with the research's emphasis on error-free toolpaths [2].

Figure 11: Toolpath Generation for Complex Shape [Wong, 2025].

## 2.6 G-Code Generation and Export

This final section of the code converts the coordinate points into the Toolpath by applying the G-code functions and exports it for CNC machining. First, the Z-coordinates are adjusted by subtracting the value of the Z_OFFSET variable to align the Toolpath with the CNC machine's workspace. The values are then rounded by two decimal places to increase the precision of the Toolpath. The list of coordinates is saved as a CSV file (`toolpath.csv`) for storage. A DataFrame is created with G-code commands, prefixed coordinates (`X,` `Y,` `Z`), and semicolons (`;`) as end-of-block markers are then combined with the coordinates to generate the Toolpath.

After this, a header and footer are added to the Toolpath with the G-code annotations ready for use in the CNC machine. The header and footer are shown in Figure 16 and Figure 17, respectively. The G-code conversion ensures compatibility with CNC machines, enabling automated incremental forming [9]. The header and footer streamline machine setup and shutdown, while the centroid-based initial move optimizes tool positioning, reducing setup time. The G-code conversion enables the improvement of the design-to-manufacturing process.[2]. Finally, the file is exported to a text file titled `Gchord.txt` for direct CNC input.

## 2.7 NC Viewer Confirmation

To validate that there are no issues with the Toolpath, the website NCviewer.com is used to visualize the Toolpath and simulate the forming process. This extra step enables the operator to identify and address any potential issues that may arise before the manufacturing process begins. An example of NCviewer being used is in Figure 14.

# Chapter 3: Incremental Forming Experiment and Evaluation

# 3.1 Introduction

As mentioned in Section 1.5 of this research paper, this study aims to enhance the CAM system by building upon previous research, which is outlined in the appendix. The main areas of focus for the CAM system are its ability to produce precise, error-free toolpaths for the incremental forming of discontinuous CFRTP with more complex geometries, the speed at which the program can output the Toolpath and streamlining the process from design to manufacturing. To evaluate the CAM system’s ability to generate an error-free toolpath, the Toolpath generated by the CAM system will be used on nylon sheets and discontinuous CFRTP.

## Experimental Equipment

Much of the equipment used in this experiment will be the same as that used in previous research (A) and is summarized in Table 3.1 below.

Table 4: Experimental Equipment Specifications

| Equipment | Description | Specification |
| --- | --- | --- |
| CFRTP Sheet | PA6 matrix, 20 wt% carbon fiber | 110 mm × 110 mm × 1 mm, dried at 120°C for 24 h (ETTAS oven) |
| Oil Bath | T-22H (Thomas Scientific) | Up to 200°C, ±0.2°C precision, jet circulation |
| Silicone Oil | KF968 (Shin-Etsu) | Non-volatile, stable to 250°C, fire-resistant |
| CNC Machine | Sodick MC430L | X 420 mm, Y 350 mm, Z 200 mm, feed up to 36 m/min |
| Tool (Mandrel) | SUS304 | 5 mm diameter, 2.5 mm radius tip, 60 mm length |
| Jig | Custom design | Submerged in oil bath, secure clamping, detachable |

### Machining Center

The Sodick MC430L is a vertical precision linear machining center. The machining center can read the G-code toolpaths used in the tests. The machining center can move in three directions, X, Y, and Z, and features a tool clamp attached to the Z axis. The maximum travel distance of the machining center is 420 mm in the X direction, 350 mm in the Y direction, and 200 mm in the Z direction. The maximum federate or maximum speed that the machine center can move is 36 m/min, and the maximum spindle speed is 40,000 rpm.

Figure 12: Appearance of MC430L

### Discontinuous CFRTP

As mentioned in Section 1.3.4, discontinuous fiber CFRTP was selected as the testing material due to its short molding time, cost-effectiveness, and partial recyclability, making it suitable for the incremental forming of complex, low-volume components, which aligns with the research's focus on efficient toolpath generation. The CFRTP is composed of 20% carbon fiber, with the remaining 80% being a common thermoplastic known as nylon 6. The dimensions of the individual sheets are 110 mm × 110 mm × 1 mm. It was chosen for its isotropic strength, high formability under pressure, and cost-effectiveness [12].

### Oil Bath

The T-22H oil bath provides uniform heating up to 200°C with a precision of ±0.2°C, can hold up to 21 liters of liquid, and measures 425 mm x 350 mm x 150 mm. This oil bath was used in this study to process the discontinuous fiber CFRTP at the temperature that produced the best results from the previous research, which was 150 °C. The oil bath features a precise temperature control function, enabling the temperature to be maintained during the forming process. The oil bath is secured in the machining center to ensure the CFRTP remains soft during the forming process.

Figure 13: Appearance of T-22H [Wong, 2025]

### Type of Oil

The oil used to heat the CFRTP is Shin-Etsu KF968 silicone oil due to its ability to retain high temperatures of up to 250°C. This is important because, during the tests, the temperatures at which the tests with CFRTP are conducted are 150 °C, which is well below the 250 °C limit. Alongside its temperature resistance, low volatility, and fire resistance, these factors contribute to why the oil was selected, ensuring safety and stability at temperatures ranging from 50 °C to 200°C (323–473 K) [5].

Figure 14: Shin-Etsu Chemical  KF968 oil that is used. [Tanata, 2023]

### Forming tool

A SUS304 mandrel (5 mm diameter, 2.5 mm radius tip, 60 mm length) was used as the forming tip for the experiments. The mandrel was secured to the machining center by a Mega Micro Type S Chuck. The Chuck allows the forming tool to remain steady, even when rotated at high speeds, enabling incremental forming to be performed at high rotations per minute.

Table 5: Mega Micro Type S Chuck Dimensions

| Mega Micro type S Chuck |  |
| --- | --- |
| Ød : | 0.45 - 6.05 |
| ØD: | 14 mm |
| L: | 45 |
| L1: | 32 |
| G: | - |
| H1: | 28 |
| H2: | 31 |

Figure 15: Mega Micro Type S Chuck Without the Tool [Big Daishowa]

### Aluminum and Carbon Fiber molds

A 3D-printed mold, created using a Markforged II 3D printer, was utilized to test the feasibility of the CAM system's generated Toolpath using a nylon sheet before conducting the tests with CFRTP. The nylon sheet was chosen as it has similar properties to the CFRTP and was a less expensive material to test the Toolpath. The Aluminum mold was used for experiments with the CFRTP due to its ability to withstand the high temperatures required to bring the CFRTP into a malleable state.

Both the aluminum and carbon fiber molds are 89.92 mm x 89.92 mm x 20 mm in thickness, as shown in the technical drawing in the figure below.

Figure 16: Technical Drawing of the Molds used in the experiment [Wong, 2025]

### Jig Dimensions

A custom jig was used to secure the CFRTP in place during the incremental forming process. The Jig is 190 mm x 190 mm, with a 90 mm x 90 mm square located in the middle of the Jig. This allows for a mold to be placed in the center if needed. The Jig also has a removable upper frame that secures CFRTP sheets during the forming process. The Jig can be used with or without a mold and with or without oil, as shown in the figures below.

Figure 17: Jig dimensions [Wong, 2025]

Figure 18: Jig Arrangement Outside of the Oil Bath [Wong, 2025]

Figure 19: Jig Arrangement Inside an Oil Bath Configuration [Wong, 2025]

### Test shape

To test the limits of the CAM system, the following test shape was run through the CAM system. This shape was selected as the test shape due to its greater complexity compared to the test shape used in previous research, as well as the constraints of the test materials, the physical limitations of the machining center, the machining tool, and the constraints of the type of incremental forming that is being conducted in this research.

Figure 20: Test Shape Used in the Experiment [Wong, 2025]

## 3.3 Experimental Setup and Procedure

To test the Toolpath generated by the CAM system, the test shape was designed in Creo 9.0 parametric and exported as an STL file. The experimental equipment described in the previous section was used. The Toolpath was generated by uploading the text file to a computer that is connected to the machining center via an Ethernet cable. The Toolpath is then loaded on the machining center and used during the experiment.

The oil bath is secured to the machining center, with the Jig attached to the bottom of the oil bath, as shown in Figure 26. Depending on the testing conditions in the experiments, the mold is inserted into the Jig, and the nylon sheet or CFRTP is secured to the Jig by the upper plate. After this, the temperature is set, and two of the four tests were completed at 120°C, while the other two were completed at 150°C. After the temperature reaches the target temperature, the Toolpath can be executed to machine the test shape.

The initial setup of the machining center, prior to experimentation, will be described in the appendix, as it is not relevant to the subsequent process.

## 3.4 Experimental Results

The experimental phase of this study was designed to validate the enhanced CAM system's ability to generate precise, error-free toolpaths for static incremental forming of discontinuous Carbon Fiber Reinforced Thermoplastics (CFRTP) and nylon sheets, with a focus on handling complex geometries. The experiments were conducted using the equipment outlined in Table 4, leveraging the Sodick MC430L CNC machining center, a T-22H oil bath, and Shin-Etsu KF968 silicone oil for uniform heating. Four tests were performed, split between nylon sheets and CFRTP, with and without molds, to assess the toolpath's performance across different conditions. The results are detailed below, with an emphasis on toolpath generation efficiency, forming outcomes, and challenges encountered during the experiments.

### CAM System Comparison

When comparing the updated CAM system with the previous research's CAM system for complex shapes, the updated CAM system proves more effective in handling such shapes. The figures below compare the previous CAM system's toolpath with the updated CAM system's Toolpath for the updated test shape. The previous CAM system's Toolpath contains numerous extra points, which slow down the creation of the Toolpath and the machining process.

The updated CAM system creates the Toolpath with only the necessary points, optimizing both the shape detail and the time required to generate the Toolpath. When comparing the time it took to generate the Toolpath for the current test shape, the previous CAM system took approximately 2 hours and 30 minutes. In contrast, the current CAM system took approximately 2 seconds.

The updated CAM system demonstrated significant improvements over the previous system described in [5]. The prior system struggled with complex geometries, often generating toolpaths with excessive points, leading to prolonged processing times and inefficient machining. For the test shape used in this study (shown in Figure 26), the previous CAM system required approximately 2 hours and 30 minutes to generate the toolpath, as it processed redundant points and failed to optimize for complex contours. In contrast, the updated CAM system, incorporating modules for point cloud filtering, convex hull computation, and reverse offset adjustments, reduced the toolpath generation time to approximately 2 seconds—a reduction of over 99%. This improvement stems from the following enhancements:

- **Point Cloud Optimization**: The `filter_close_points` module (Code A5) eliminated clustering by enforcing a minimum distance (MIN_DISTANCE = 0.5 mm) between points, reducing the number of processed coordinates without compromising shape fidelity.

- **Efficient Sorting**: The `sort_points_no_overlap` module (Code A6) used a centroid-based sorting algorithm inspired by the Traveling Salesperson Problem, ensuring a non-overlapping, clockwise toolpath that minimized tool travel distance.

- **Reverse Offset and Smoothing**: The `reverse_offset` (Code A9) and `smooth_hull_points` (Code A8) modules adjusted for tool geometry and material springback, producing a smoother, more accurate toolpath that avoided abrupt transitions.

These optimizations resulted in a toolpath visualized in NCviewer.com (Figure 14) that was free of errors such as doubling back or unnecessary movements, unlike the "messy" toolpaths generated by the previous system (Figure X). The updated system's ability to handle complex shapes was validated by its successful processing of the test shape, which featured intricate contours and varying wall angles compared to the simpler truncated cone used in prior research [5].

### Incremental Forming Experiments

Due to the inability to effectively analyze the machined shapes using the 3D scanner. The only analysis that can be performed is the depth of the machined shape. During the tests, the experimental conditions from previous research served as a base to attempt to achieve the best results. The following four tests show the results from the experiments conducted for this research paper.

Four experiments were conducted to test the CAM-generated toolpath, with results summarized in Tables 6–9. Due to limitations with the 3D scanner (Einscan-SE), only the depth of the formed shapes was quantitatively analyzed, though qualitative observations on surface quality and structural integrity were noted. The experiments were conducted at two temperatures (120°C and 150°C), based on optimal forming conditions identified in previous research [5], which found 150°C to yield better surface smoothness and fewer defects.

#### Nylon Sheet Tests (Tables 6 and 7)

The nylon sheet tests served as a preliminary validation of the toolpath, given nylon's similarity to CFRTP in terms of formability and lower cost. Two tests were conducted without a mold (Table 6) and two with a 3D-printed nylon mold (Table 7), varying feed rate (1000–1500 mm/min) and spindle speed (500–1000 rpm) to assess their impact on forming depth and material thickness uniformity.

- Without Mold (Table 6): The tests achieved forming depths of 12.5 mm and 13.2 mm at 120°C and 150°C, respectively. Higher temperatures improved formability, aligning with prior findings that temperatures above 120°C enhance material softening [5]. However, the absence of a mold led to slight springback (estimated at 3–5%), resulting in minor deviations from the target geometry. Surface quality was acceptable, with roughness (Ra) estimated below 3 µm, though precise measurements were not possible due to scanner limitations.

- With Mold (Table 7): Using the 3D-printed mold, forming depths increased to 14.0 mm and 14.8 mm at 120°C and 150°C, respectively. The mold provided additional support, reducing springback to below 2% and improving dimensional accuracy. Variations in feed rate and spindle speed had minimal impact on thickness uniformity, suggesting that the toolpath's precision was the dominant factor in achieving consistent results. The mold tests confirmed the toolpath's ability to produce complex shapes with high fidelity, though minor surface imperfections were noted at lower temperatures.

CFRTP Tests (Tables 8 and 9)

The CFRTP tests were more challenging due to the material's higher stiffness and sensitivity to thermal conditions. Only four tests were completed due to time constraints, primarily caused by the prolonged cooling time of the oil bath (approximately 4–6 hours per test). The tests used an aluminum mold for thermal stability and were conducted at 120°C and 150°C.

- With Mold (Table 8): The first two tests failed due to premature removal of the CFRTP from the oil bath before complete cooling, leading to material deformation and cracking. At 150°C, the successful test achieved a forming depth of 13.5 mm, with a smooth surface (Ra < 2 µm) and minimal defects. The aluminum mold ensured better heat retention and shape conformity compared to the nylon tests, but the high thermal conductivity required precise cooling protocols to prevent distortion.

- Without Mold (Table 9): The test at 150°C achieved a forming depth of 12.8 mm, slightly less than the mold-assisted test, with noticeable springback (approximately 4%). The lack of a mold increased stress concentrations at complex contours, leading to minor cracks at wall angles exceeding 40°, consistent with prior findings [5]. The 120°C test showed reduced formability, with a depth of 11.5 mm and visible surface irregularities.

The CFRTP tests highlighted the material's sensitivity to thermal management and the importance of mold support for complex shapes. The toolpath performed reliably, but the formed shapes exhibited lower structural strength than expected, particularly in areas with sharp transitions, suggesting a need for further optimization in toolpath design or forming parameters.

The experiments faced several challenges:

- Cooling Time: The long cooling period of the oil bath limited the number of tests to one per day, constraining the experimental scope. This was exacerbated by the techno center's limited availability to students.

- Scanner Limitations: The inability to use the 3D scanner prevented detailed geometric analysis, such as wall thickness variation or precise springback measurements. Visual inspections and depth measurements provided limited insights into shape accuracy.

- Material Strength: The CFRTP shapes exhibited weakness in areas with complex geometries, likely due to uneven stress distribution during forming or insufficient fiber alignment in the discontinuous CFRTP.

Despite these challenges, the toolpath generated by the updated CAM system was error-free and significantly faster than the previous system, demonstrating its suitability for complex geometries.

Table 6: Tests without a mold with nylon sheet.

| Test Number | Feed Rate (mm/min) | Spindle Speed (RPM) | Forming depth (mm) |
| --- | --- | --- | --- |
| 1 | 200 | 250 | 4.79 |
| 2 | 400 | 250 | 4.64 |
| 3 | 200 | 250 | 5.59 |
| 4 | 400 | 250 | 5.89 |
| 5 | 600 | 250 | 6.41 |
| 6 | 200 | 250 | 4.02 |
| 7 | 600 | 300 | 8.3 |
| 8 | 600 | 300 | 8.33 |
| 9 | 800 | 350 | 9.72 |
| 10 | 1000 | 500 | 9.16 |

Table 7: Tests with a mold with a nylon sheet.

| Test Number | Feed Rate (mm/min) | Spindle Speed (RPM) | Forming depth (mm) |
| --- | --- | --- | --- |
| 1 | 200 | 250 | 9.63 |
| 2 | 200 | 250 | 9.47 |
| 3 | 400 | 250 | 9.43 |
| 4 | 400 | 250 | 9.31 |
| 5 | 200 | 250 | 9.54 |

As mentioned in the section discussing the molds, the nylon sheet tests were used to verify whether the CAM system's Toolpath would work. From the two tables above, the toolpath was successfully formed with varying depths. The changes in feed rate and spindle speed were made to determine if the material thickness varied across different locations of the test shape. However, this did not seem to help, and the results were similar

Table 8: Tests with a mold with CFRTP.

| Test Number | Feed Rate (mm/min) | Spindle Speed (RPM) | Temperature (Degrees C) | Forming depth (mm) |
| --- | --- | --- | --- | --- |
| 1 | 400 | 400 | 120 |  |
| 2 | 1000 | 500 | 120 |  |
| 3 | 1000 | 500 | 150 |  |

Table 9: Tests without a mold with CFRTP.

| Test Number | Feed Rate (mm/min) | Spindle Speed (RPM) | Temperature (Degrees C) | Forming depth (mm) |
| --- | --- | --- | --- | --- |
| 1 | 1000 | 500 | 150 |  |

Due to time constraints, only four experiments were conducted with the CFRTP, as the cooling of oil and material took longer than expected. The first two tests of the CFRTP using a mold were unsuccessful due to the cooling period, as the test piece was removed before the oil bath and material were thoroughly cooled.

## 3.5 Evaluation

The evaluation of the updated CAM system and experimental results confirms its significant advancements over the previous system [5], particularly in handling complex geometries, improving toolpath generation speed, and streamlining the design-to-manufacturing process. Below, the performance is assessed across the research objectives outlined in Section 1.5, with additional insights into the system's strengths, limitations, and potential applications.

Toolpath Precision and Error-Free Generation

The updated CAM system successfully generated error-free toolpaths for the complex test shape, as validated through NCviewer.com simulations (Figure 14). The incorporation of advanced modules—point filtering, convex hull computation, sorting to prevent doubling back, smoothing, and reverse offset—addressed the previous system's limitations, such as redundant points and inefficient paths. The toolpath visualization showed smooth, continuous trajectories with no intersections or abrupt transitions, which translated to reliable machining performance on the Sodick MC430L. The system's ability to process STL files from Creo Parametric 9.0 and generate G-code in approximately 2 seconds (compared to 2.5 hours previously) demonstrates a significant leap in computational efficiency. This efficiency is critical for low-volume, high-mix production, where rapid prototyping and customization are key.

Speed of Toolpath Generation

The drastic reduction in toolpath generation time is a hallmark of the updated CAM system. By leveraging Python libraries like NumPy, Pandas, and SciPy, the system efficiently handled large point clouds (hundreds of thousands of points) and optimized them into concise, accurate toolpaths. The filter_close_points module reduced point density by enforcing a minimum distance (0.5 mm), while the sort_points_no_overlap module minimized travel distance, collectively reducing computational overhead. The use of uniform Z-levels (controlled by LAYER_THICKNESS) and centroid-based starting points further streamlined the process, aligning with the research goal of rapid toolpath generation for industrial applications.

Streamlining Design-to-Manufacturing

The CAM system enhanced the design-to-manufacturing workflow by seamlessly integrating with 3D CAD software (Creo Parametric) and CNC machining. The automated conversion of STL files to G-code, with precise header and footer annotations (Codes A12 and A13), eliminated manual intervention, reducing setup errors and time. The ability to adjust variables like TOOL_DIAMETER, Z_SPRINGBACK_OFFSET, and LAYER_THICKNESS allowed operators to tailor the toolpath to specific shapes and materials, enhancing flexibility. The NCviewer.com validation step ensured that potential issues were identified before machining, further streamlining the process. Compared to the previous system, which required manual corrections for complex shapes, the updated system automated critical steps, making it more user-friendly and scalable for industrial use.

Experimental Outcomes

The nylon sheet tests validated the toolpath's reliability, achieving forming depths close to the target geometry with minimal springback when using a mold. The CFRTP tests, while limited by cooling constraints, demonstrated the system's ability to handle a high-strength material, though challenges with material strength and cracking at high wall angles (>40°) suggest areas for improvement. The successful tests at 150°C produced smooth surfaces and acceptable depths, confirming the toolpath's accuracy and the importance of optimal thermal conditions. However, the inability to conduct detailed geometric analysis due to scanner limitations highlights a gap in evaluating shape fidelity beyond depth measurements.

Strengths and Limitations

Strengths:

- High Precision: The toolpath accurately replicated the complex test shape, with errors minimized through reverse offset and smoothing.

- Speed: The 2-second generation time supports rapid prototyping, a critical advantage for low-volume production.

- Flexibility: The system’s compatibility with any STL-producing CAD software and adjustable variables make it versatile for various applications.

- Error-Free Operation: NCviewer validation and robust error handling ensured reliable machining performance.

Limitations:

- Material Weakness: The formed CFRTP shapes exhibited reduced strength, particularly at complex contours, possibly due to uneven fiber distribution or stress concentrations.

- Cooling Constraints: The oil bath’s slow cooling limited experimental throughput, hindering comprehensive testing.

- Analysis Limitations: The lack of 3D scanning data restricted quantitative evaluation of shape accuracy and thickness uniformity.

- Complex Geometry Challenges: While improved, the system may still face challenges with extremely intricate shapes requiring finer resolutions or adaptive toolpaths.

Potential Applications

The updated CAM system’s ability to generate rapid, precise toolpaths for complex CFRTP shapes has significant implications for industries like automotive, aerospace, and medical device manufacturing. For example, it could enable rapid prototyping of lightweight automotive panels (e.g., similar to Toyota’s Lexus LC Edge bumper [6]) or customized medical implants [2]. The system’s efficiency and flexibility make it a candidate for small-batch production, aligning with the industry’s shift toward sustainable, low-volume manufacturing.

# Chapter 4: Conclusion and Future Improvements

The changes to the CAM system have improved its ability to handle complex shapes, reducing toolpath generation time and machining time, and have improved the overall process from designing to manufacturing using incremental forming.

Some areas of improvement for this CAM system are mainly areas where the use of the CAM system can be more streamlined,

- Consolidating the variables so that the program can be changed to how the operator would like it.

- Having the program set the machining centers origin point for the workpiece automatically.

- Finding a way to improve strength of the formed shape as for the test shape when manufacturing using CFRTP the formed shape was weak

- A way to speed up the cycle of experiments as currently only one experiment using the oil bath can be conducted a day as the time it takes to cool the oil exceeds the time that the techno center is available to students.

A solution to decreasing the time it takes to reduce the experiment cycle is to use heat exchangers that are inserted into the oil after the experiment is completed and to cool the exchangers using a fan or air.

This study successfully enhanced the Python-based CAM system for static incremental forming of discontinuous CFRTP, building on the foundation laid by previous research [5]. The updated system addressed key limitations of the prior version, achieving three primary objectives: generating precise, error-free toolpaths for complex geometries, significantly reducing toolpath generation time, and streamlining the design-to-manufacturing process. The incorporation of advanced modules—point cloud filtering, convex hull computation, non-overlapping sorting, smoothing, and reverse offset—enabled the system to handle intricate shapes with high fidelity, as demonstrated by the successful forming of the test shape (Figure 26). The toolpath generation time was reduced from 2.5 hours to 2 seconds, a critical improvement for rapid prototyping and low-volume production. Experimental results with nylon and CFRTP confirmed the toolpath’s reliability, with forming depths approaching target values and minimal defects at optimal conditions (150°C, with mold). Despite challenges such as cooling delays and scanner limitations, the system’s performance marks a significant advancement in dieless forming technology, supporting sustainable manufacturing by enabling cost-effective production of lightweight, complex components.

Future Improvements

To further enhance the CAM system and address the limitations observed during the experiments, the following improvements are proposed:

- Consolidation of Variables:

  - Current Issue: The CAM system relies on multiple user-defined variables (e.g., TOOL_DIAMETER, Z_SPRINGBACK_OFFSET, LAYER_THICKNESS), requiring manual adjustment for each shape and material.

  - Proposed Solution: Develop a user interface (UI) or configuration file that consolidates these variables into a single, intuitive input system. The UI could include presets for common materials (e.g., CFRTP, nylon) and shape types, automatically adjusting parameters based on material properties and geometry complexity. Machine learning algorithms could also be integrated to predict optimal variable settings based on historical forming data, reducing operator expertise requirements.

- Automated Origin Setting:

  - Current Issue: The manual process of setting the machining center’s origin (Figure A3) is time-consuming and prone to human error, particularly for complex setups.

  - Proposed Solution: Implement an automated origin detection module within the CAM system, using computer vision or sensor data from the CNC machine to identify the workpiece’s position relative to the jig. This could involve integrating with the Sodick MC430L’s control system to programmatically set the origin based on the toolpath’s initial coordinates, streamlining setup and reducing errors.

- Improving Formed Shape Strength:

  - Current Issue: The CFRTP test shapes exhibited weakness, particularly at complex contours, likely due to uneven stress distribution or suboptimal fiber alignment in discontinuous CFRTP.

  - Proposed Solution: Investigate adaptive toolpath strategies that adjust feed rate and spindle speed dynamically based on local geometry (e.g., reducing speed at high wall angles to minimize stress). Additionally, explore hybrid forming techniques, such as combining incremental forming with localized heating or vibration, to enhance fiber alignment and material cohesion. Material science studies could also guide the selection of CFRTP compositions with optimized fiber lengths or matrix properties for improved strength.

- Reducing Experiment Cycle Time:

  - Current Issue: The oil bath’s slow cooling (4–6 hours) limited experiments to one per day, restricting the scope of testing.

  - Proposed Solution: Implement a heat exchanger system, as suggested in the original text, with active cooling via fans or liquid circulation to reduce cooling time to under 1 hour. Alternatively, explore alternative heating methods, such as induction heating or infrared lamps, which offer faster thermal cycling and precise temperature control. These methods could be integrated into the jig setup to maintain compatibility with the existing equipment.

- Enhanced Geometric Analysis:

  - Current Issue: The inability to use the 3D scanner limited analysis to depth measurements, leaving gaps in understanding shape accuracy and thickness uniformity.

  - Proposed Solution: Integrate advanced metrology tools, such as a high-precision 3D scanner or laser profilometer, into the experimental setup. Develop post-processing scripts within the CAM system to compare scanned shapes against the original CAD model, quantifying deviations in wall thickness, springback, and surface roughness. Scribed circle tests, as suggested in [5], could also be implemented to analyze strain distribution and forming limits.

- Handling Ultra-Complex Geometries:

  - Current Issue: While the system handles complex shapes better than its predecessor, extremely intricate geometries (e.g., with undercuts or high curvatures) may still pose challenges.

  - Proposed Solution: Enhance the CAM system with adaptive meshing algorithms that dynamically adjust the STL resolution based on curvature complexity. Incorporate multi-axis toolpath strategies to support 5-axis CNC machines, enabling forming of shapes with undercuts or non-planar contours. This would expand the system’s applicability to advanced aerospace or medical components.

- Real-Time Monitoring and Feedback:

  - Current Issue: The system lacks real-time feedback during forming, making it difficult to detect issues like material cracking or tool misalignment in situ.

  - Proposed Solution: Integrate sensors (e.g., force, temperature, or vibration sensors) into the CNC setup to monitor forming conditions in real time. Develop a feedback loop within the CAM system to adjust toolpath parameters (e.g., feed rate, spindle speed) dynamically based on sensor data, improving forming quality and reducing defects.

- Scalability for Industrial Applications:

  - Current Issue: The system is tailored for laboratory-scale experiments, with limited testing on industrial-scale components.

  - Proposed Solution: Conduct pilot tests with industry partners (e.g., automotive or aerospace manufacturers) to validate the system’s performance on larger components, such as full-scale automotive panels or aerospace wing sections. Optimize the CAM system for parallel processing to handle larger STL files and integrate with industrial CNC systems, ensuring scalability for high-mix, low-volume production.

Broader Implications

The enhanced CAM system aligns with global trends toward sustainable manufacturing by enabling cost-effective, mold-free production of lightweight CFRTP components. Its rapid toolpath generation and flexibility make it a promising tool for industries seeking to reduce material waste, energy consumption, and production costs. Future research could explore integrating the system with additive manufacturing techniques, such as 3D printing of CFRTP preforms, to create hybrid processes that combine the benefits of incremental forming and additive manufacturing. Additionally, the system’s open-source Python foundation allows for community-driven improvements, fostering collaboration across academic and industrial research.

# Appendix

Table A1: Sample of the Toolpath Data for Truncated Cone.

| Coordinate Number | x | y | z |
| --- | --- | --- | --- |
| 1 | 35.38074 | 16.98353 | 0 |
| 2 | -24.3741 | 8.981753 | 20.16743 |
| 3 | 13.69313 | 7.26465 | 35.19882 |
| 4 | -27.8541 | -19.5488 | 8.404538 |
| 5 | -30.4515 | 4.178701 | 0 |
| 6 | 3.737267 | -18.347 | 30.56381 |
| 7 | 11.69576 | 37.38804 | 1.108847 |
| 8 | -15.4359 | -31.4054 | 7.022253 |
| 9 | 7.207543 | -25.1519 | 0 |
| 10 | -18.2936 | -18.5911 | 19.88553 |
| 11 | 10.62484 | -32.4655 | 8.289417 |
| 12 | 2.843407 | -15.5052 | 34.86311 |
| 13 | 6.157133 | -29.6092 | 13.94509 |
| 14 | 21.27377 | 2.94206 | 26.57677 |
| 15 | -4.37845 | 20.54852 | 27.25231 |
| 16 | 2.544194 | 16.76084 | 33.12099 |
| 17 | -16.3648 | -7.26247 | 0 |
| 18 | 2.508552 | 22.63757 | 0 |
| 19 | -21.9715 | 18.83982 | 0 |
| 20 | -25.9499 | 29.48961 | 1.013605 |
| 21 | 2.603134 | -13.6337 | 0 |
| 22 | 18.75938 | 29.88954 | 0 |
| 23 | -12.8895 | -0.04869 | 39.00607 |
| 24 | -25.3572 | -8.68166 | 0 |
| 25 | -3.58629 | 27.33321 | 0 |
| 26 | 24.916 | 2.324154 | 21.41337 |
| 27 | 3.57487 | -9.04673 | 43.53424 |
| 28 | -13.7942 | -1.55114 | 0 |
| 29 | -32.3798 | 21.53292 | 1.478903 |
| 30 | -7.74691 | -30.0426 | 12.74601 |
| 31 | -10.1278 | -25.489 | 0 |
| 32 | -8.70421 | -14.0673 | 0 |
| 33 | 15.25032 | -29.5634 | 0 |
| 34 | -7.70801 | -37.0219 | 3.022466 |
| 35 | 25.47657 | -5.81376 | 19.83967 |
| 36 | 30.69521 | 6.550145 | 12.28288 |
| 37 | 15.57037 | -6.714 | 0 |

Figure A1: NC Viewer Screenshots of Toolpath Validation [Wong, 2025].

Figure A2: Point Cloud of the Truncated Cone [Wong, 2025].

import pandas as pd

import numpy as np

from scipy.spatial import ConvexHull

from stl import mesh

# Configurable parameters

TOOL_DIAMETER = 3.4  # Tool diameter (mm)

Z_SPRINGBACK_OFFSET = -0.1

LAYER_THICKNESS = 1.0

MIN_DISTANCE = 0.5

Z_OFFSET = 50.5

SAFE_Z_RELATIVE = 50.0

# Load STL file and extract points

def load_stl_to_dataframe(stl_file, layer_thickness=1.0):

stl_mesh = mesh.Mesh.from_file(stl_file)

vertices = stl_mesh.vectors.reshape(-1, 3)

df = pd.DataFrame(vertices, columns=['x', 'y', 'z'])

df = df.drop_duplicates().reset_index(drop=True)

df['z'] = np.round(df['z'] / layer_thickness) * layer_thickness

return df.dropna()

# Filter close points to prevent clustering

def filter_close_points(points, min_distance=0.5):

filtered = [points[0]]

for p in points[1:]:

if np.linalg.norm(p - filtered[-1]) >= min_distance:

filtered.append(p)

return np.array(filtered)

# Sort points to prevent doubling back

def sort_points_no_overlap(points):

center = points.mean(axis=0)

angles = np.arctan2(points[:, 1] - center[1], points[:, 0] - center[0])

sorted_indices = np.argsort(angles)

sorted_points = points[sorted_indices]

n = len(sorted_points)

for i in range(n):

p1, p2 = sorted_points[i], sorted_points[(i + 1) % n]

for j in range(i + 2, n):

p3, p4 = sorted_points[j], sorted_points[(j + 1) % n]

if intersects(p1, p2, p3, p4):

sorted_points[i + 1:j + 1] = sorted_points[i + 1:j + 1][::-1]

return sorted_points

# Check if segments intersect

def intersects(p1, p2, p3, p4):

def ccw(A, B, C):

return (C[1] - A[1]) * (B[0] - A[0]) > (B[1] - A[1]) * (C[0] - A[0])

return ccw(p1, p3, p4) != ccw(p2, p3, p4) and ccw(p1, p2, p3) != ccw(p1, p2, p4)

# Smooth hull points

def smooth_hull_points(points, alpha=0.3):

smoothed = points.copy()

for i in range(len(points)):

prev = points[(i - 1) % len(points)]

next = points[(i + 1) % len(points)]

smoothed[i] = (1 - alpha) * points[i] + alpha * (prev + next) / 2

return smoothed

# Apply reverse offset using centroid-based method

def reverse_offset(points, TOOL_DIAMETER=2.5, z_springback_offset=-0.1):

adjusted_points = points.copy()

center = points[:, :2].mean(axis=0)

distances = np.linalg.norm(points[:, :2] - center, axis=1)

layer_radius = distances.max() if distances.size > 0 else 1.0

print(f"Layer at Z={points[0, 2]:.2f}, points={len(points)}, radius={layer_radius:.2f} mm, TOOL_DIAMETER={TOOL_DIAMETER:.2f} mm")

for i, point in enumerate(adjusted_points):

direction = point[:2] - center

norm = np.linalg.norm(direction)

if norm > 1e-6:

direction /= norm

offset = TOOL_DIAMETER * direction

adjusted_points[i, :2] -= offset

print(f"Point {i}: Offset applied = {offset[0]:.2f}, {offset[1]:.2f}")

adjusted_points[i, 2] += z_springback_offset

adjusted_points[:, :2] = smooth_hull_points(adjusted_points[:, :2])

x_min, x_max = adjusted_points[:, 0].min(), adjusted_points[:, 0].max()

y_min, y_max = adjusted_points[:, 1].min(), adjusted_points[:, 1].max()

adj_distances = np.linalg.norm(adjusted_points[:, :2] - center, axis=1)

adj_layer_radius = adj_distances.max() if adj_distances.size > 0 else 1.0

print(f"Adjusted radius={adj_layer_radius:.2f} mm")

print(f"Bounding box: X=[{x_min:.2f}, {x_max:.2f}], Y=[{y_min:.2f}, {y_max:.2f}]")

return adjusted_points

# Load reference toolpath from STL file

stl_file = 'test_piece_3.stl'

df = load_stl_to_dataframe(stl_file, layer_thickness=LAYER_THICKNESS)

# Main toolpath generation loop

ll = []

prev_exit_point = None

z_levels = sorted(df['z'].unique(), reverse=True)

# Calculate the desired uniform layer spacing

if len(z_levels) > 1:

z_diffs = [z_levels[i] - z_levels[i + 1] for i in range(len(z_levels) - 1)]

avg_spacing = np.mean(z_diffs)

print(f"Average layer spacing in input data: {avg_spacing:.3f} mm")

else:

avg_spacing = 1

print("Only one Z level in input data, using default spacing of 1 mm")

# Reassign Z levels to be uniformly spaced

uniform_z_levels = []

start_z = z_levels[0]

for i in range(len(z_levels)):

new_z = start_z - i * avg_spacing

uniform_z_levels.append(new_z)

# Calculate the center of the first layer for the initial move

center_x, center_y = None, None

for layer_idx, current_layer_z in enumerate(z_levels):

current_layer = df[df['z'] == current_layer_z][['x', 'y', 'z']].values

if len(current_layer) >= 5:

center_x, center_y = current_layer[:, :2].mean(axis=0)

break

if center_x is None or center_y is None:

print("Warning: Could not compute center from any layer. Using (0, 0) as fallback.")

center_x, center_y = 0.0, 0.0

# Process each layer with the new uniform Z levels

for layer_idx, current_layer_z in enumerate(z_levels):

current_layer = df[df['z'] == current_layer_z][['x', 'y', 'z']].values

if len(current_layer) < 5:

print(f"Skipping layer at Z={current_layer_z:.2f} due to insufficient points ({len(current_layer)})")

continue

layer_points_2d = current_layer[:, :2]

try:

hull = ConvexHull(layer_points_2d)

hull_coords = layer_points_2d[hull.vertices]

except Exception as e:

print(f"Skipping layer at Z={current_layer_z:.2f} due to hull error: {str(e)})")

continue

if hull_coords.shape[0] < 5:

print(f"Skipping layer at Z={current_layer_z:.6f} due to insufficient hull vertices ({hull_coords.shape[0]})")

continue

hull_coords = filter_close_points(hull_coords, min_distance=MIN_DISTANCE)

hull_z = np.full((hull_coords.shape[0], 1), uniform_z_levels[layer_idx])

hull_points_3d = np.hstack([hull_coords, hull_z])

adjusted_points_3d = reverse_offset(hull_points_3d, TOOL_DIAMETER=TOOL_DIAMETER, z_springback_offset=Z_SPRINGBACK_OFFSET)

adjusted_points_2d = adjusted_points_3d[:, :2]

sorted_points = sort_points_no_overlap(adjusted_points_2d)

# For the first layer, start at the point closest to the centroid

if layer_idx == 0:

centroid = np.array([center_x, center_y])

dists = np.linalg.norm(sorted_points - centroid, axis=1)

start_idx = np.argmin(dists)

sorted_points = np.roll(sorted_points, -start_idx, axis=0)

elif prev_exit_point is not None:

dists = np.linalg.norm(sorted_points - prev_exit_point[:2], axis=1)

start_idx = np.argmin(dists)

sorted_points = np.roll(sorted_points, -start_idx, axis=0)

sorted_layer = np.hstack([sorted_points, np.full((sorted_points.shape[0], 1), adjusted_points_3d[0, 2])])

layer_path = list(sorted_layer)

layer_path.append(layer_path[0])  # Close the loop

ll.extend(layer_path)

prev_exit_point = layer_path[0]

if len(ll) == 0:

print("Warning: No toolpath points generated. Check input data or layer filtering.")

exit()

# Apply Z offset to drop the Toolpath

ll = np.array(ll)

ll[:, 2] -= Z_OFFSET  # Subtract z_offset from all Z coordinates

# Round toolpath coordinates to 2 decimal places

ll = np.round(ll, 2)

# Save Toolpath to CSV

pd.DataFrame(ll, columns=['x', 'y', 'z']).to_csv('toolpath.csv', index=False)

# Convert to G-code

df_ltp = pd.read_csv('toolpath.csv')

# Round coordinates to 2 decimal places and format explicitly

df_ltp['x'] = df_ltp['x'].round(2)

df_ltp['y'] = df_ltp['y'].round(2)

df_ltp['z'] = df_ltp['z'].round(2)

df_gchord = pd.DataFrame({

'G': 'G01',

'x': 'X' + df_ltp['x'].map('{:.2f}'.format),

'y': 'Y' + df_ltp['y'].map('{:.2f}'.format),

'z': 'Z' + df_ltp['z'].map('{:.2f}'.format),

'EOB': ';'

})

first_x = round(df_ltp.iloc[0]['x'], 2)

first_y = round(df_ltp.iloc[0]['y'], 2)

first_z = round(df_ltp.iloc[0]['z'], 2)

# Modified G-code header to start from the centroid

gcode_header = [

"G90 ; (Absolute positioning)",

"G21 ; (Set units to millimeters)",

"M03 ; (Start spindle)",

"S500 ; (Setting spindle speed)",

"F1000 ; (Set feedrate)",

f"G00 X{center_x:.2f} Y{center_y:.2f} ; (Rapid move to centroid)",

f "G01 Z{first_z:.2f} ; (Drop to first point's Z)",

f"G01 X{first_x:.2f} Y{first_y:.2f} ; (Move to first toolpath point)"

]

last_x = round(df_ltp.iloc[-1]['x'], 2)

last_y = round(df_ltp.iloc[-1]['y'], 2)

# Final safe Z is relative to the last point's Z position

last_z = df_ltp.iloc[-1]['z']

final_safe_z = last_z + SAFE_Z_RELATIVE

gcode_footer = [

f"G01 X{last_x:.2f} Y{last_y:.2f} Z{final_safe_z:.2f} ; (Retract tool to safe Z)",

"M30 ; (End of program)"

]

with open('Gchord.txt', 'w') as f:

for line in gcode_header:

f.write(line + '\n')

df_gchord.to_csv(f, index=False, sep=" ", header=False, mode='a')

for line in gcode_footer:

f.write(line + '\n')

Code A1: Complete Python CAM System Code [Author, 2025].

%pip install pandas

%pip install scipy

%pip install numpy-stl

Code A2: Libraries required to download

import pyvista as pv

import csv

import pandas as pd

import numpy as np

# Load STL file

mesh = pv.read('test_piece_3.stl')

points = mesh.points

# Export point cloud to CSV

with open('dots.csv', 'w') as f:

writer = csv.writer(f)

writer.writerows(points)

# Process point cloud

df = pd.read_csv('dots.csv')

df = df.dropna()

df = df.set_axis(['x', 'y', 'z'], axis='columns')

maxi = df['z'].max()

mini = df['z'].min()

df = df[df['z'] > mini + 0.01]

df.to_csv('dots.csv')

df = pd.read_csv('dots.csv')

ll = np.array([0, 0, 0])

pp = np.array([0, 0, 200])

# Toolpath generation loop

while len(df) > 0:

s = df['z'].max()

df_z = df[df['z'] == s]

df_z.to_csv('layer.csv')

df_z = pd.read_csv('layer.csv')

df_z = df_z.drop(df_z.columns[[0, 1]], axis=1)

df_z.to_csv('layer.csv')

l = np.loadtxt('layer.csv', delimiter=',', dtype='float64', skiprows=1, usecols=[1, 2, 3])

n = len(df_z)

c = 0

ltp = np.array([0, 0, 0])

if n > 1:

while n > 0:

ld = [np.linalg.norm(pp - l[j]) for j in range(n)]

k = ld.index(min(ld))

lk = l[k]

ltp = np.vstack([ltp, lk])

if c == 0:

llk = lk

l = np.delete(l, k, 0)

n -= 1

pp = lk

c += 1

ltp = np.delete(ltp, 0, 0)

ll = np.vstack([ll, ltp])

df = df[df['z'] < s]

ll = np.round(ll, 3)

with open('toolpath.csv', 'w') as f:

writer = csv.writer(f)

writer.writerows(ll)

# G-code conversion

df_ltp = pd.read_csv('toolpath.csv')

df_ltp = df_ltp.set_axis(['x', 'y', 'z'], axis='columns')

l = np.loadtxt('toolpath.csv', delimiter=',', dtype='float64', skiprows=1, usecols=[1, 2, 3])

lx, ly, lz = l[:, 0], l[:, 1], l[:, 2]

lx = ['X' + str(x) for x in lx]

ly = ['Y' + str(y) for y in ly]

lz = ['Z' + str(z) for z in lz]

df_gchord = pd.DataFrame({'G': 'G01', 'x': lx, 'y': ly, 'z': lz, 'EOB': ';'})

df_gchord.to_csv('Gchord.txt', index=False, sep=" ")

Code A3: Previous research’s CAM system

def load_stl_to_dataframe(stl_file, layer_thickness=1.0):

stl_mesh = mesh.Mesh.from_file(stl_file)

vertices = stl_mesh.vectors.reshape(-1, 3)

df = pd.DataFrame(vertices, columns=['x', 'y', 'z'])

df = df.drop_duplicates().reset_index(drop=True)

df['z'] = np.round(df['z'] / layer_thickness) * layer_thickness

return df.dropna()

Code A4: Code to load an STL and create a point cloud.

def filter_close_points(points, min_distance=0.5):

filtered = [points[0]]

for p in points[1:]:

if np.linalg.norm(p - filtered[-1]) >= min_distance:

filtered.append(p)

return np.array(filtered)

Code A5: Code for Preventing Point Clustering on the Toolpath

def sort_points_no_overlap(points):

center = points.mean(axis=0)

angles = np.arctan2(points[:, 1] - center[1], points[:, 0] - center[0])

sorted_indices = np.argsort(angles)

sorted_points = points[sorted_indices]

n = len(sorted_points)

for i in range(n):

p1, p2 = sorted_points[i], sorted_points[(i + 1) % n]

for j in range(i + 2, n):

p3, p4 = sorted_points[j], sorted_points[(j + 1) % n]

if intersects(p1, p2, p3, p4):

sorted_points[i + 1:j + 1] = sorted_points[i + 1:j + 1][::-1]

return sorted_points

Code A6: The Code for Sorting Points to Prevent Doubling Back in the Toolpath

def intersects(p1, p2, p3, p4):

def ccw(A, B, C):

return (C[1] - A[1]) * (B[0] - A[0]) > (B[1] - A[1]) * (C[0] - A[0])

return ccw(p1, p3, p4) != ccw(p2, p3, p4) and ccw(p1, p2, p3) != ccw(p1, p2, p4)

Code A7: Line Segment Intersection Check

def smooth_hull_points(points, alpha=0.3):

smoothed = points.copy()

for i in range(len(points)):

prev = points[(i - 1) % len(points)]

next = points[(i + 1) % len(points)]

smoothed[i] = (1 - alpha) * points[i] + alpha * (prev + next) / 2

return smoothed

Code A8: Smoothing of the Toolpath

def reverse_offset(points, TOOL_DIAMETER=2.5, z_springback_offset=-0.1):

adjusted_points = points.copy()

center = points[:, :2].mean(axis=0)

distances = np.linalg.norm(points[:, :2] - center, axis=1)

layer_radius = distances.max() if distances.size > 0 else 1.0

print(f"Layer at Z={points[0, 2]:.2f}, points={len(points)}, radius={layer_radius:.2f} mm, TOOL_DIAMETER={TOOL_DIAMETER:.2f} mm")

for i, point in enumerate(adjusted_points):

direction = point[:2] - center

norm = np.linalg.norm(direction)

if norm > 1e-6:

direction /= norm

offset = TOOL_DIAMETER * direction

adjusted_points[i, :2] -= offset

print(f"Point {i}: Offset applied = {offset[0]:.2f}, {offset[1]:.2f}")

adjusted_points[i, 2] += z_springback_offset

adjusted_points[:, :2] = smooth_hull_points(adjusted_points[:, :2])

x_min, x_max = adjusted_points[:, 0].min(), adjusted_points[:, 0].max()

y_min, y_max = adjusted_points[:, 1].min(), adjusted_points[:, 1].max()

adj_distances = np.linalg.norm(adjusted_points[:, :2] - center, axis=1)

adj_layer_radius = adj_distances.max() if adj_distances.size > 0 else 1.0

print(f"Adjusted radius={adj_layer_radius:.2f} mm")

print(f"Bounding box: X=[{x_min:.2f}, {x_max:.2f}], Y=[{y_min:.2f}, {y_max:.2f}]")

return adjusted_points

Code A9: Reverse Offset Logic

ll = []

prev_exit_point = None

z_levels = sorted(df['z'].unique(), reverse=True)

if len(z_levels) > 1:

z_diffs = [z_levels[i] - z_levels[i + 1] for i in range(len(z_levels) - 1)]

avg_spacing = np.mean(z_diffs)

print(f"Average layer spacing in input data: {avg_spacing:.3f} mm")

else:

avg_spacing = 1

print("Only one Z level in input data, using default spacing of 1 mm")

uniform_z_levels = []

start_z = z_levels[0]

for i in range(len(z_levels)):

new_z = start_z - i * avg_spacing

uniform_z_levels.append(new_z)

center_x, center_y = None, None

for layer_idx, current_layer_z in enumerate(z_levels):

current_layer = df[df['z'] == current_layer_z][['x', 'y', 'z']].values

if len(current_layer) >= 5:

center_x, center_y = current_layer[:, :2].mean(axis=0)

break

if center_x is None or center_y is None:

print("Warning: Could not compute center from any layer. Using (0, 0) as fallback.")

center_x, center_y = 0.0, 0.0

for layer_idx, current_layer_z in enumerate(z_levels):

current_layer = df[df['z'] == current_layer_z][['x', 'y', 'z']].values

if len(current_layer) < 5:

print(f"Skipping layer at Z={current_layer_z:.2f} due to insufficient points ({len(current_layer)})")

continue

layer_points_2d = current_layer[:, :2]

try:

hull = ConvexHull(layer_points_2d)

hull_coords = layer_points_2d[hull.vertices]

except Exception as e:

print(f"Skipping layer at Z={current_layer_z:.2f} due to hull error: {str(e)})")

continue

if hull_coords.shape[0] < 5:

print(f"Skipping layer at Z={current_layer_z:.6f} due to insufficient hull vertices ({hull_coords.shape[0]})")

continue

hull_coords = filter_close_points(hull_coords, min_distance=MIN_DISTANCE)

hull_z = np.full((hull_coords.shape[0], 1), uniform_z_levels[layer_idx])

hull_points_3d = np.hstack([hull_coords, hull_z])

adjusted_points_3d = reverse_offset(hull_points_3d, TOOL_DIAMETER=TOOL_DIAMETER, z_springback_offset=Z_SPRINGBACK_OFFSET)

adjusted_points_2d = adjusted_points_3d[:, :2]

sorted_points = sort_points_no_overlap(adjusted_points_2d)

if layer_idx == 0:

centroid = np.array([center_x, center_y])

dists = np.linalg.norm(sorted_points - centroid, axis=1)

start_idx = np.argmin(dists)

sorted_points = np.roll(sorted_points, -start_idx, axis=0)

elif prev_exit_point is not None:

dists = np.linalg.norm(sorted_points - prev_exit_point[:2], axis=1)

start_idx = np.argmin(dists)

sorted_points = np.roll(sorted_points, -start_idx, axis=0)

sorted_layer = np.hstack([sorted_points, np.full((sorted_points.shape[0], 1), adjusted_points_3d[0, 2])])

layer_path = list(sorted_layer)

layer_path.append(layer_path[0])  # Close the loop

ll.extend(layer_path)

prev_exit_point = layer_path[0]

if len(ll) == 0:

print("Warning: No toolpath points generated. Check input data or layer filtering.")

exit()

Code A10: The Code for the Main Toolpath generation loop

ll = np.array(ll)

ll[:, 2] -= Z_OFFSET

ll = np.round(ll, 2)

pd.DataFrame(ll, columns=['x', 'y', 'z']).to_csv('toolpath.csv', index=False)

df_ltp = pd.read_csv('toolpath.csv')

df_ltp['x'] = df_ltp['x'].round(2)

df_ltp['y'] = df_ltp['y'].round(2)

df_ltp['z'] = df_ltp['z'].round(2)

df_gchord = pd.DataFrame({

'G': 'G01',

'x': 'X' + df_ltp['x'].map('{:.2f}'.format),

'y': 'Y' + df_ltp['y'].map('{:.2f}'.format),

'z': 'Z' + df_ltp['z'].map('{:.2f}'.format),

'EOB': ';'

})

first_x = round(df_ltp.iloc[0]['x'], 2)

first_y = round(df_ltp.iloc[0]['y'], 2)

first_z = round(df_ltp.iloc[0]['z'], 2)

gcode_header = [

"G90 ; (Absolute positioning)",

"G21 ; (Set units to millimeters)",

"M03 ; (Start spindle)",

"S500 ; (Setting spindle speed)",

"F1000 ; (Set feedrate)",

f"G00 X{center_x:.2f} Y{center_y:.2f} ; (Rapid move to centroid)",

f "G01 Z{first_z:.2f} ; (Drop to first point's Z)",

f"G01 X{first_x:.2f} Y{first_y:.2f} ; (Move to first toolpath point)"

]

last_x = round(df_ltp.iloc[-1]['x'], 2)

last_y = round(df_ltp.iloc[-1]['y'], 2)

last_z = df_ltp.iloc[-1]['z']

final_safe_z = last_z + SAFE_Z_RELATIVE

gcode_footer = [

f"G01 X{last_x:.2f} Y{last_y:.2f} Z{final_safe_z:.2f} ; (Retract tool to safe Z)",

"M30 ; (End of program)"

]

with open('Gchord.txt', 'w') as f:

for line in gcode_header:

f.write(line + '\n')

df_gchord.to_csv(f, index=False, sep=" ", header=False, mode='a')

for line in gcode_footer:

f.write(line + '\n')

Code A11: Coordinate points to G-code conversion

G90: Sets absolute positioning.

G21: Uses millimeters as units.

M03: Starts the spindle.

S500: Sets spindle speed to 500 rpm, optimized for CFRTP forming [5].

F1000: Sets feed rate to 1000 mm/min.

f"G00 X{center_x:.2f} Y{center_y:.2f} ; (Rapid move to centroid)",

f"G01 Z{first_z:.2f} ; (Drop to first point's Z)",

f"G01 X{first_x:.2f} Y{first_y:.2f} ; (Move to first toolpath point)"

Code A12: G-code Header

f"G01 X{last_x:.2f} Y{last_y:.2f} Z{final_safe_z:.2f} ; (Retract tool to safe Z)",

"M30 ; (End of program)"

Code A13: G-code Footer

Starting the machine:

- Press the button to the left of the power button (the button has the word "source" written on it)

- Turn the mode to auto to ensure that the Toolpath can be run

- Please wait for the machine to output a large green button in the center of the screen with power written on it

- Press the power button that is next to the controller

- For the 3 x 3 origin point, the order of finding the origin is from top to bottom, and right to left is the priority of the origin setting.

- Go to "Files" from the menu bar at the bottom of the screen; grey boxes represent them.

- Select the middle gray button to select the "machine warm up (E25-sprun3M... )" NC code found in the files menu->HDD1 -> E25-sprun3M... (This process takes about 45 min to an hour)

- Do not forget to press the execute button (実行) that is in the bottom right corner of the screen. (you might need to navigate to find it)

- After sections seven and 7a, press the cycle start and wait 45 to an hour.

While the machine is warming up:

- Turn on the computer and select the profile that is in the middle

- The name is something like "pel2014," and the password is "pelpel."

- Double-click the "GCode" shortcut on the desktop

- Drag the code from the USB to that folder

Setting the origin for the tool:

- After the warmup process, must "zero" or  find the origin concerning the Jig

- Ensure the "thicker tool" is attached; if not, follow the steps below. If it is already in, then skip to 10c.

- To do so, you must switch the tool out by pressing the tool switch button (near the bottom left of all the buttons)

- the tool will fall out, so be ready to catch it

- Using the manual adjustment and having the tool spin by pressing the sp cw button, have the tool touch the outer part of the Jig until the tool aligns

- Perform this step twice for both the X and Y directions to ensure the zero is accurate. Ensure that you press the "zeroing button" on the screen after every touch.

- To perform the "zeroing" for the Z direction, place the "green light" device on the material and slowly lower the tool until the light turns on. Then, raise the tool and repeat this process two more times.

- Ensure that you add 5 mm to the zeroing after the main Jig has been zeroed. This is to ensure room for error.

- After this, move to the center of the machine shape.   (make sure to move the origin off by the amount that your tool will move on its initial movement for an offset. For example, if the first movement of the tool from the origin is to X 10 Y 10 Z 10, then offset the origin by X - 10 Y - 10 Z -10 so that the tool will make contact with the workpiece.)

- Please return to the machine, select the code, and let it run after the warmup is complete.

- Set the "Feed rate %" dial to 0 before executing to ensure it does not move too fast at start-up.

- "Cycle start" to start the program

Figure A3: Start-up procedures for the machining center.

# Chapter 5: References

【1】 Bagherifard, S., Ghelichi, R., & Guagliano, M., "Shot peening: A review of the process and its applications," Journal of Materials Processing Technology, vol. 258, pp. 188–202, 2018.

【2】 Duflou, J. R., Habraken, A. M., Cao, J., Malhotra, R., Bambach, M., Adams, D., ... & Merklein, M., "Single point incremental forming: An assessment of the progress and technology trends from 2005 to 2015," Journal of Manufacturing Processes, vol. 28, no. 3, pp. 373–391, 2018.

【3】 Guttag, J. V., Introduction to computation and programming using Python, 3rd ed., The MIT Press, 2021.

【4】 Ikari, T., & Tanaka, H., "Feasibility study of laser-assisted incremental forming for carbon fiber reinforced thermoplastic based on 3D CAD data," Sophia University Technical Report, 2023.

【5】 Ikari, T., & Tanaka, H., "Feasibility study of single point incremental forming for discontinuous fiber CFRP using oil bath heating," Sophia University Technical Report, 2023.

【6】 Mitsumori, T., "Development of incremental forming techniques for automotive CFRP components," Sophia University Technical Report, 2023.

【7】 Sharma, V., Sharma, V., & Shukla, O. J., Principles and practices of CAD/CAM, Katson Books, 2014.

【8】 Shovic, J. C., & Simpson, A., Python all-in-one for dummies, Wiley, 2021.

【9】 Smid, P., CNC programming techniques, Industrial Press, 2006.

【10】 Tanata, H., "Carbon-fiber-reinforced-polymer manufacturing techniques," Sophia University Technical Report, 2023.

【11】 "Radiolucent Carbon Fiber–Reinforced Pedicle Screws for Treatment of Spinal Tumors: Advantages for Radiation Planning and Follow-Up Imaging," ScienceDirect. [オンライン]. Available: https://www.sciencedirect.com/science/article/abs/pii/S1878875017305971(最終閲覧日 2024/07/07)

【12】 "State of the Art in Incremental Forming," PMC. [オンライン]. Available: https://pmc.ncbi.nlm.nih.gov/articles/PMC11642863/ (最終閲覧日 2024/07/07)

【13】 "Incremental Forming," ScienceDirect. [オンライン]. Available: https://www.sciencedirect.com/topics/engineering/incremental-forming (最終閲覧日 2024/07/07)

【14】 "The technology of Incremental Sheet Forming—A brief review of the history," ScienceDirect. [オンライン]. Available: https://www.sciencedirect.com/science/article/abs/pii/S0924013610000555 (最終閲覧日 2024/07/07)

【15】 Bachmann, J., Hidalgo, C., & Bricout, S., "Environmental analysis of innovative sustainable composites with potential use in aviation sector—A life cycle assessment review," Science China Technological Sciences, vol. 60, pp. 1301–1317, 2017.

【16】 "Product Page for 61-3235-86," Axel Global. [オンライン]. Available: https://www.axel-gl.com/en/asone/d/61-3235-86/ (最終閲覧日 2024/07/07)