S0:

Hello. My name is Karter Wong, and I will be presenting my research topic: the Development of CAM systems for the Incremental Forming of CFRTP from 3D CAD data.

S1:

Today, I will briefly review some background information, the previous research on the topic, the progress that I have made during this past year, a brief overview of the Experiment, the result, and finally summarize the findings and improvements that can be made for this research topic

S2:

So, what is Incremental forming?

Incremental forming is a flexible forming process that can shape sheets of various materials using plastic deformation of the sheet with a tool into the desired shape.

Unlike traditional manufacturing processes, it does not require dies or molds, making it ideal for low-volume production, prototyping, or custom parts. The tool follows a programmed path to manufacture shell shapes, offering reduced setup and production costs.

It also allows the production of various products in small quantities, where mold creation would be too expensive.

S3:

An example of Incremental forming in use today is by car manufacturers like Ford, Nissan, and Lexus. These manufacturers use incremental forming to prototype new vehicle designs and add minor customizations to vehicles, as seen on the Lexus LC edge, as shown here.

S4:

My research is based on a previous research project that developed a simple Python-based CAM system that could generate a tool path and conducted experiments to test the tool path.

The CAM system developed during the previous research can be described in four steps:

First, STL data from the 3D CAD data is converted into a point cloud, a collection of points from the triangles given by the STL file.

Next, the point cloud's points are grouped into layers defined by the Z coordinate. During this process, the program looks for the points on the outermost part of the figure so that the toolpath is not generated with unnecessary movements.

Third, the toolpath is calculated by calculating the distances from the tool's current position to the other points on the layer and moving to the point with the shortest distance. This process is repeated for each layer of the shape.

The final step is to convert the X, Y, and Z coordinates into G-code so that a CNC machine can read the generated tool path and manufacture a product.

S5:

The CAM system, while effective for simple shapes, had limitations when applied to more complex shapes. These included generating inefficient toolpaths with unnecessary tool movements, long toolpath generation times, and an overall inefficient workflow to go from design to manufacturing. The changes made to the CAM system in this research study address these issues.

S6:

The enhancements to the CAM system can be categorized into nine key areas, visualized in these boxes, which address the issues previously mentioned.

The top six boxes, focus on point management; new sections of code were added to filters and remove duplicate or invalid points that could skew the path; sorted points more efficiently by the Z coordinate; introduced rounding mechanisms to enhance positional accuracy; removing layers with fewer than five points; and optimized the toolpath generation to minimize unnecessary loops or jumps.

The bottom-left box handles CNC-specific criteria such as a tool's diameter, compensates for material springback, and considers the physical limits of the machining center, such as travel ranges and safety boundaries.

Finally, the last two boxes enhance usability and users can now customize the G-code output based on specific equipment or experimental conditions, and the system automatically adds the initial setup commands and termination sequences, speeding up the experimental process.

S7:

To evaluate these changes to the CAM system, a more challenging test shape was used instead of the truncated cone used in the prior research.

The new shape is a rectangular prism with chamfered and rounded edges, measuring 30 mm by 30 mm by 9.9 mm thick. These dimensions were chosen to fit within the CNC machine, ensure no sharp 90-degree angles, introduce sufficient complexity to stress-test the path generation, and mimic real-world parts.

S8:

When generating the toolpath for this test shape, the updated CAM system significantly reduced toolpath generation time from the previous research's 2.5 hours to 2 seconds. The toolpaths of both CAM systems were simulated using NCviewer to check for any toolpath errors.

As you can see from the figures, the previous CAM system adds a lot of unnecessary points to the toolpath, causing an increased generation time.

S9:

With the tool path verified, the incremental forming trials using an MC430L machining center could begin. The workpiece was a 110 mm by 110 mm by 1 mm sheet of CFRTP, secured over a custom mold measuring 89.92 mm by 89.92 mm by 20 mm. The forming tool used was a 5 mm diameter rod, as shown here.

S10:

For the CFRTP experiments, a T-22 H oil bath system was used to uniformly and precisely heat the silicon oil and CFRTP to the required temperature. The jig, holding the mold, is mounted at the bath's base, with the CFRTP sheet secured to the jig.

This controlled heating is needed for the incremental forming of CFRTP, as its formability is better when heated, allowing for deeper forming depths and better shape retention compared to room-temperature processing.

S11:

In this study, four types of incremental forming tests were done—tests using nylon sheets and discontinuous CFRTP as materials, and both with and without the mold. The nylon trials were used to prove toolpath feasibility and won't be explained, as the focus is on CFRTP performance.

The feed rate and spindle speed are based on the previous research's experimental conditions. The first test here has a slower speed as a safety measure, as it was the first test that was done with the heated oil bath.

For CFRTP, four tests were performed under varying conditions, as shown on the slide. The two at 120 degrees Celsius had rough surfaces and fracturing because the sheets were removed from the oil bath too early, causing uneven cooling. The 150-degree tests succeeded in achieving near-target depths with smooth finishes.

Due to technical issues with our 3D scanner, a detailed analysis was limited, so the only measurement taken was the forming depth, as it was the only one that could be taken accurately.

S12:

A visual side-by-side comparison of the CFRTP results with and without the mold shows advantages to using a mold: The max depth of a test with a mold was 10.8 mm, exceeding the 9.9 mm target depth, and preserved the geometry with higher fidelity. The non-molded test, while successfully formed, underformed in curved areas.

These results confirm that the upgraded CAM system can generate reliable tool paths for complex CFRTP geometries.

S13:

In summary, the changes made to the previous CAM system solved several issues, such as generating precise tool paths for intricate shapes, reducing generation times to near-instantaneous levels, and simplifying the workflow for faster prototyping.

The forming depths averaged within a 5% margin of error, with the molds having less error. The 150°C temperature proved optimal, consistent with earlier findings. However, this data set is small, so the data may not be accurate.

S14:

That said, there are further improvements to be made. On the CAM side, additional optimizations could include automated origin detection for the workpiece and jig, accelerating setup times by eliminating manual alignment, which currently slows down experiments.

Experimentally, developing a way to cool the oil bath would enable multiple tests per day, as the current cooldown period restricts experiments to one a day.

Lastly, getting a 3D scanner would allow comprehensive post-forming analysis, including thickness uniformity and geometric deviation metrics, for deeper insights.

S15-17:

Here are the key citations supporting this work. Thank you for your attention