Progress Report

2025/06/09 Karter Wong

Progress

- Completed several experiments for incremental forming on nylon sheets with and without a mold

金型の有無にかかわらずナイロンシートの増分成形に関するいくつかの実験を完了しました

- Tested out various spindle speeds and feed rates for incremental forming with and without a mold

金型の有無にかかわらず、増分成形のさまざまなスピンドル速度と送り速度をテストしました

| Test number | Feed Rate (mm/min) | Spindle Speed (RPM) | Successful forming of the shape? | Notes |
| --- | --- | --- | --- | --- |
| 1 | 200 | 250 | Yes | Areas around the formed shape were visibly thin. |
| 2 | 200 | 250 | Yes | Similar results to the first test |
| 3 | 400 | 250 | Yes | Shift the workpiece origins by adding 0.5 mm to the Y axis |
| 4 | 400 | 250 | Yes | Similar results to the 3rd test |
| 5 | 200 | 250 | Yes | Reduced the toolpath by 3.9 mm to make sure that the spindle would not touch the mold during forming. |

Table 1: Test with mold

| Test number | Feed Rate (mm/min) | Spindle Speed (RPM) | Successful formation of the shape? | Notes |
| --- | --- | --- | --- | --- |
| 1 | 200 | 250 | No | Due to the machining center's soft limit, the top portion that holds the nylon sheet needs to be raised to run the toolpath program. |
| 2 | 400 | 250 | No | The shape is vague; there is little to no depth. Shifted the workpiece origin by 0.5 mm in the Z direction |
| 3 | 200 | 250 | No | Like test 2, also shifted the workpiece origin in the Z direction |
| 4 | 400 | 250 | No | It is formed deeper than test 3, but it is still not at the desired depth. Will lower by 0.4 mm |
| 5 | 600 | 250 | Yes | Less forming depth than the previous tests |
| 6 | 20 | 50 | Yes | It still has a vague shape, but a little deeper, and the workpiece origin was lowered by 1.3 mm for a total of 2.5 mm from the Z origin set. |
| 7 | 600 | 300 | Yes | Lowered the workpiece by 0.9 mm from the experiment 6 for a total of 3.4 mm. Better results, getting closer to the results of with the mold. |

Table 2: Test without mold

- During the experiments with the mold, there were better results due to the reduced spring back from the sheet when pushed down by the spindle during formation.

金型を使った実験では、成形中にスピンドルで押し下げられたときにシートからの跳ね返りが減少したため、より良い結果が得られました。

- For the experiments without the mold, it was harder to form as the spring back would be higher. This resulted in needing a higher feed rate and spindle speed, so the nylon would stay in the forming shape.

金型を使用しない実験では、スプリングバックが大きく、成形が困難でした。そのため、ナイロンを成形形状に保つために、送り速度とスピンドル回転速度を上げる必要がありました。

Plan

- Continue to conduct tests without a mold to try to reduce the spring back and reach the desired depth by increasing the spindle speed and the feed rate

金型なしでテストを継続し、スピンドル速度と送り速度を上げることでスプリングバックを減らし、希望の深さに到達するようにします。

  - If I get good results this week, I will discuss with Professor Tanaka about the next steps and working with CFRTP

今週良い結果が得られたら、田中教授と次のステップとCFRTPの活用について話し合います。

- Work on my graduation thesis and my midterm presentation

卒業論文と中間発表に取り組む